Farm and Ranch Flat Industrial Alkyd Enamel

Product Description

A high quality, low VOC, high solids, interior/exterior alkyd paint characterized by excellent durability and color retention.

Where to Use

This product is a heavy-duty enamel designed for architectural and industrial maintenance applications on wood or steel substrates. Not for use directly on galvanized steel or zinc.

Product Characteristics

Color	Black

Gloss	Flat

Architectural and Industrial

Maintenance Category	Industrial Maintenance Coatings

| Temperature | To Touch | To Recoat |
| --- | --- | --- |
| 75°F / 55% R.H. | 3 Hours | 8 hours |

Drying Time

(Cooler temperatures and higher humidity will lengthen drying time)

Preparation & Priming

Surface Preparation	For maximum performance, the recommended substrate should be blasted in accordance with SSPC-SP7.  If blast cleaning is not feasible, the substrate should be degreased in accordance with SSPC-SP1.  All burrs should be removed and sharp edges or rough weld seams should be ground down.  Full use should then be made of mechanical power tools, in conjunction with wire brushing and chipping to remove all loose rust and mill scale to a standard of cleanliness conforming to SP-2 or SP-3.  Prior to painting, all dust should be removed from the substrate by using clean brushes and/or dry compressed air.

Primer Coats	For best results on steel Anchor’s Farm and Ranch Rust Inhibitive Series Primers are recommended.

Mixing & Application

Mixing	Stir thoroughly, making sure no pigment remains on the bottom of the can.

Thinning	This coating is VOC compliant; only thin if permitted by federal, state and local regulations.  If necessary, use Anchor FR1131 Synthetic Reducer, Mineral Spirits, or Xylene.

Surface Temperature	Minimum 50°F, Maximum 110°F - The surface should be dry and the relative humidity should be no greater than 85%.

Recommended Thickness	1.6-2.0 mils dry per coat, two coats recommended

Theoretical Coverage	844 ft2/gallon at 1 mil dry, assuming no application loss.  Coverage will vary depending on color, surface texture and application technique.

|  | Dry Mils | Wet Mils | Ft2/Gal |
| --- | --- | --- | --- |
| Suggested | 1.8 | 3.4 | 468 |
| Minimum | 1.6 | 3.0 | 528 |
| Maximum | 2.0 | 3.8 | 422 |

Coverage Rates per Coat

| Airless Spray | Pressure | 1200-2200 psi |
| --- | --- | --- |
|  | Tip | 0.011"-0.015" |
| Conventional Spray | Air Pressure | 40-70 psi |
|  | Fluid Pressure | 10-20 psi |
| Roller | Use 1/4" synthetic nap covers. |  |
| Brush | Use high quality natural china bristle brushes. |  |

Application Equipment

Application Considerations	May be applied by brush, roller, conventional, or airless spray.  To avoid dusting, apply in wet coats.  On a derusted surface, the application of a dry film thickness of at least 2 mils is recommended.  Faster dry time may be obtained with increased air movement and/or higher substrate or material temperature.

Application: Use with FR1100 Urethane Convertor:

When used with Anchor FR1100 Urethane Convertor; mix at a ratio of 8:1. The optimal blend is 8 parts of Farm and Ranch Industrial Alkyd Enamel to 1 part FR1100. In actual use this is one gallon of Farm and Ranch Alkyd Enamel and one pint of FR1100 Polyurethane Convertor.

The following table gives the expected dry times associated with application:

| (All time in Hours) | w/o FR1100 | With 8:1 FR1100 |
| --- | --- | --- |
| Dry to Touch | 4 | 2.5 |
| Tack Free | 5 | 4.5 |
| Dry Through | 24 | 24 |

Clean-up & Storage

Cleanup	Use Anchor FR1131, Mineral Spirits, or Xylene

Storage Temperature	Minimum 20°F			Maximum 110°F

Shelf Life	Under Normal Conditions (Unopened) – Two Years

Safety & Important Information

DANGER!  FLAMMABLE LIQUID AND VAPOR.  VAPOR HARMFUL.  CONTAINS:  MINERAL SPIRITS AND N-BUTYL ACETATE.  Vapor harmful.  May affect the brain or nervous system causing dizziness, headache or nausea.  Causes nose, eye, skin and throat irritation.  Harmful if swallowed.  NOTICE:  Reports have associated repeated and prolonged occupational overexposure to solvents with permanent brain and nervous system damage.  Intentional misuse by deliberately concentrating and inhaling the contents may be harmful or fatal.

Keep away from heat, sparks and flame.  Vapors may cause flash fire.  Do not smoke.  Extinguish all flames and pilot lights, and turn off stoves, heaters, electric motors and other sources or ignition during use and until all vapors are gone.  Prevent build-up of vapors by opening all windows and doors to achieve cross-ventilation.  Use only with adequate ventilation.  Do not breathe vapors or spray mist.  Ensure fresh air entry during application and drying.  If you experience eye watering, headache or dizziness or if air monitoring demonstrates vapor/mist levels are above applicable limits, wear an appropriate, properly fitted respirator (NIOSH approved) during and after application.  Follow respirator manufacturer’s directions for respirator use.  Do not get in eyes, on skin or clothing.  Wash thoroughly after handling.  KEEP OUT OF REACH OF CHILDREN.

WARNING! If you scrape, sand or remove old paint, you may release lead dust. LEAD IS TOXIC. EXPOSURE TO LEAD DUST CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN. PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE. Wear a NIOSH-approved respirator to control lead exposure. Clean up carefully with a HEPA vacuum and a wet mop. Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead. WARNING! Sanding or scraping pressure treated lumber may be hazardous; wear appropriate protection.

VERSION: 07/2025

LIMITED WARRANTY:  The technical data on this label or on other data is true and accurate to the best of our knowledge.  We guarantee our products to conform to ANCHOR PAINT MFG. CO. quality control standards.  Due to misuse in handling, storage, application and workmanship or variables such as weather or surface integrity that are beyond our control, Anchor Paint does not authorize any representative to make any warranty or merchantability of fitness of this product.  Any liability whatsoever of Anchor Paint Mfg. Co. to the buyer or user of this product is limited to the purchaser’s cost of the product itself.

Farm and Ranch Industrial Flat Alkyd Enamel

Product Description

General Description	A high quality, low VOC, high solids, interior/ exterior alkyd resin coating characterized by excellent durability and color retention.

Common Usage	This product is a heavy-duty enamel designed for architectural and industrial maintenance applications.

Color	Black

Finish

Technical Data

Flat

Solids by Volume	53%

Recommended Thickness	1.6-2.0 mils dry per coat, two coats recommended

| Temperature | To Touch | To Recoat |
| --- | --- | --- |
| 75°F / 55% R.H. | 3 Hours | 8 hours |

Drying Time

(Cooler temperatures and higher humidity will lengthen drying time)

Architectural and Industrial

Maintenance Category	Industrial Maintenance Coatings

AIM Category VOC Limit	3.7 lb/gal (443 g/l)

Actual VOC	3.17 lb/gal (380 g/l)

Density	11.21 lb/gal (1343 g/l)

Theoretical Coverage	844 ft2/gallon at 1 mil dry, assuming no application loss.  Coverage will vary depending on color, surface texture and application technique.

Packaging	55 Gallon drums, 5 Gallon pails, 1 Gallon cans

Storage Temperature	Minimum 20°F			Maximum 110°F

Chemical Resistance	Alkalis:  Fair		Acids:  Good		Water:  Good

Safety	Refer to Product Data Sheet or SDS for safety information.

Performance Data

Substrate	Steel

Surface Preparation	SSPC-SP10

System Tested	One coat FR0900 Farm and Ranch Industrial Alkyd Enamel White or one coat FR0900 Farm and Ranch Industrial Alkyd Enamel White with FR1100 Polyurethane Converter (8:1)

| Test Name | Test Method | FR0900 | FR0900 + FR1100 |
| --- | --- | --- | --- |
| QUV | ASTM D-4587 – 312 Hours | Retain 31.5% 20° Gloss and 69% 60° Gloss | Retain 61% 20° Gloss and 84% 60° Gloss |
| Salt Fog Resistance | ASTM B117 | 250 Hours | 225 Hrs |
| Hardness (Pencil) | ASTM D 3363 | 4B | HB |
| Adhesion (Pulloff)* | ASTM D 4541 | 650 PSI | 600 PSI |
| Adhesion (Crosshatch) | ASTM D 3359 | 4B | 4B |
| Direct Impact | ASTM D-2794 | 50 inch/pounds | 10 inch/pounds |

*Pull-off Adhesion testing conducted with one coat 0991 Saf-T-Gard II Base 1 or one coat 0991 Saf-T-Gard II Base 1 with J1100 Urethane Converter (8:1)

VERSION: 07/2025

LIMITED WARRANTY:  The technical data on this label or on other data is true and accurate to the best of our knowledge.  We guarantee our products to conform to ANCHOR PAINT MFG. CO. quality control standards.  Due to misuse in handling, storage, application and workmanship or variables such as weather or surface integrity that are beyond our control, Anchor Paint does not authorize any representative to make any warranty or merchantability of fitness of this product.  Any liability whatsoever of Anchor Paint Mfg. Co. to the buyer or user of this product is limited to the purchaser’s cost of the product itself.