Polyurethane Converter – FR1100

Product Description

An aliphatic polyisocyanate to be mixed with compatible alkyds to increase gloss, hardness and chemical resistance and to accelerate drying, curing and chemical cross-linking.

Where to Use

This product may be used for applications where light exposure to acids, alkalis, salt, most solvents and water is evident.

Product Characteristics

Color	Clear Amber

Gloss	Gloss

Architectural and Industrial

Maintenance Category	Not intended for residential use; Shop use only

Preparation & Priming

Surface Preparation	Follow the surface preparations of the coating to which FR1100 is being added.

Primer Coats	After mixing FR1100 with the appropriate alkyd and properly preparing the surface it may be used as a finish coat over alkyd primers, acrylics, polyamide epoxies, urethanes, vinyls and direct to substrate.

Mixing & Application

Mixing	For Anchor Farm and Ranch Industrial Alkyd Enamel thoroughly mix 8 parts paint with one part FR1100 Polyurethane Convertor by volume. (One gallon paint to one pint FR1100)

For Anchor Farm and Ranch Quick Dry Industrial Alkyd Enamel mix 16 parts paint with one part FR1100 Polyurethane Convertor by volume. (One gallon paint to one half pint FR1100)

Limitations	The addition of more converter than recommended may shorten pot life and cause coating to become excessively brittle.  Not recommended for submersion or for exposures where temperatures exceed more than 275°F continuously. For use with Anchor Farm and Ranch Industrial Alkyd Enamels only.

Recommended Thickness	Follow the recommendations of the coating to which FR1100 is being added.

Pot Life	8 hours

Application Considerations	Follow the recommendations of the coating to which FR1100 is being added.

Technical Information

Solids by Volume	80.00%

Actual VOC	3.06 lb/gal (367 g/l)

Density	8.75 lb/gal (1138 g/l)

Packaging	1 Gallon cans, and pint (1/8 gallon) cans

Clean-up & Storage

Cleanup	Use Anchor FR1131, mineral spirits, or xylene.

Storage Temperature	Minimum 32°F			Maximum 122°F

FR1100 Polyurethane Hardener should be tightly sealed and stored where it is protected from heat, moisture, and foreign materials.  Recommended storage temperatures are 50-80°F.  Temperatures above this may cause material to polymerize or container to burst.  It is recommended that the contents be used as soon as possible after opening as contamination may cause material to solidify.

Moisture Sensitivity	This product is moisture sensitive.  To avoid contamination with atmospheric moisture keep container closed until ready for use.

Shelf Life	Under Normal Conditions (Unopened) – Two Years

Safety & Important Information

DANGER!  VAPOR AND SPRAY MIST HARMFUL.  OVEREXPOSURE MAY CAUSE LUNG DAMAGE.  MAY CAUSE ALLERGIC SKIN AND RESPIRATORY REACTION, EFFECTS MAY BE PERMANENT.  MAY AFFECT THE BRAIN OR NERVOUS SYSTEM CAUSING DIZZINESS, HEADACHE OR NAUSEA.  CAUSES EYE, SKIN, NOSE AND THROAT IRRITATION.  FLAMMABLE LIQUID AND VAPOR.  CONTAINS: ALIPHATIC DIISOCYANTES AND PETROLEUM DISTILLATES.  NOTICE:  Reports have associated repeated and prolonged occupational overexposure to solvents with permanent brain and nervous system damage.  Intentional misuse by deliberately concentrating and inhaling the contents may be harmful or fatal.

INDIVIDUALS WITH LUNG OR BREATHING PROBLEMS OR PRIOR REACTION TO ISOCYANATES MUST NOT BE EXPOSED TO VAPOR OR SPRAY MIST.  Do not breathe vapor or spray mist.  Wear an appropriate, properly fitted respirator (NIOSH approved) during application unless air monitoring demonstrates vapor/mist levels are below applicable limits.  An airline respirator (NIOSH approved) is recommended.  A vapor/particulate respirator (NIOSH approved) may be appropriate where airborne monitoring demonstrates vapor levels below ten time the applicable exposure limits.  Follow respirators manufacturer’s directions for respirator use.

Do not get in eyes, on skin or clothing.  Wash thoroughly after handling.  Keep away from heat, sparks and flam.  Vapor may cause flash fire.  Use only with adequate ventilation.  KEEP OUT OF REACH OF CHILDREN.

WARNING! If you scrape, sand or remove old paint, you may release lead dust. LEAD IS TOXIC. EXPOSURE TO LEAD DUST CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN. PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE. Wear a NIOSH-approved respirator to control lead exposure. Clean up carefully with a HEPA vacuum and a wet mop. Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead. WARNING! Sanding or scraping pressure treated lumber may be hazardous; wear appropriate protection.

Version: 07/2025

LIMITED WARRANTY:  The technical data on this label or on other data is true and accurate to the best of our knowledge.  We guarantee our products to conform to ANCHOR PAINT MFG. CO. quality control standards.  Due to misuse in handling, storage, application and workmanship or variables such as weather or surface integrity that are beyond our control, Anchor Paint does not authorize any representative to make any warranty or merchantability of fitness of this product.  Any liability whatsoever of Anchor Paint Mfg. Co. to the buyer or user of this product is limited to the purchaser’s cost of the product itself.