House and Barn Exterior Acrylic Latex Primer

Product Description

A 100% acrylic exterior latex primer; this coating is effective at resisting staining and discoloration caused by tannins in most woods.  Some woods such as redwood and cedar may contain excessive amounts of tannins resulting in stain bleed-through. A second coat of FR3601 may be used in this case. Any tannin bleed should be encapsulated by the first coat and will not bleed into the second.

Where to Use

For use on properly prepared surfaces such as wood, masonry, asphalt, steel, galvanized, and other metals. FR3601 may also be used on other surfaces such as glass, tile, and some plastics. Test on a small area for adhesion to your substrate before use.

Product Characteristics

Color	White

Gloss	Low Sheen

Architectural and Industrial

Maintenance Category	Primers and Undercoaters

| Temperature | To Touch | To Recoat |
| --- | --- | --- |
| 75°F / 55% R.H. | 1 hour | 2 hours |

Drying Time

(Cooler temperatures and higher humidity will lengthen drying time)

Preparation & Priming

Surface Preparation	Paint only over clean and dry surfaces.  Remove all loose paint, oil, grease, dirt, chalk or other contaminants that would hinder the performance of the coating.  Mildew must be killed by scrubbing with a solution of a non-soapy detergent such as T.S.P. (Tri-Sodium Phosphate), household bleach and warm water. Thoroughly rinse affected area and let dry prior to painting.  Repair all damaged areas and repair any cracks or splits with appropriate caulk or filler.  Glossy surfaces should be sanded.  On unfinished porous surfaces such as concrete block, a block filler should be used prior to priming.

Finish Coats	This product is designed for use as a primer for Anchor House and Barn Exterior Acrylic Latex, as well as most other interior and exterior flat through gloss latex paints.

Mixing & Application

Mixing	Stir thoroughly, making sure no pigment remains on the bottom of the can.

Thinning	Thin with water only if necessary, up to one pint per gallon

Surface Temperature	Minimum 50°F, Maximum 110°F - The surface should be dry and the relative humidity should be less than 85%.

Recommended Thickness	1.6-2.0 mils dry

|  | Dry Mils | Wet Mils | Ft2/gal |
| --- | --- | --- | --- |
| Suggested | 1.8 | 3.4 | 345 |
| Minimum | 1.6 | 3.0 | 388 |
| Maximum | 2.0 | 3.8 | 311 |

Theoretical Coverage	621 ft2/gallon at 1 mil dry, assuming no application losses.  Coverage will vary depending on color, the surface texture and application technique.

Coverage Rates per Coat

| Airless Spray | Pressure | 1800-2400 psi |
| --- | --- | --- |
|  | Tip | 0.015"-0.017" |
| Conventional Spray | Air Pressure | 40-70 psi |
|  | Fluid Pressure | 10-20 psi |
| Roller | Use a 3/8" or a 1/2" synthetic roller cover. |  |
| Brush | Use high quality synthetic or nylon bristle brushes. |  |

Application Equipment

Application Considerations	This coating allows for brush, roller, or spray application.  Always apply into rather than away from the wet edge, overlapping each pass 50%.  Avoid touching up, rolling or brushing back into paint more than ten minutes after applying.  Touch up when paint is completely dry.  Allow the paint to cure at least ten days before cleaning newly painted surfaces.

Clean-up & Storage

Cleanup	Use soap and water

Storage Temperature	Minimum 35°F			Maximum 110°F

Shelf Life	Under Normal Conditions (Unopened) – Two Years

Safety & Important Information

Contains ethylene glycol. See SDS for important safety information.

Use only with adequate ventilation.  Avoid breathing vapors or spray mist.  Ensure fresh air entry during application and drying.  If you experience eye watering, headache or dizziness or if air monitoring demonstrates vapor/mist levels are above applicable limits, wear an appropriate, properly fitted respirator (NIOSH approved) during and after application.  Follow respirator manufacturer’s directions for respirator use.  Avoid contact with eyes.  Wash thoroughly after handling.  KEEP OUT OF REACH OF CHILDREN.

WARNING! If you scrape, sand or remove old paint, you may release lead dust. LEAD IS TOXIC. EXPOSURE TO LEAD DUST CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN. PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE. Wear a NIOSH-approved respirator to control lead exposure. Clean up carefully with a HEPA vacuum and a wet mop. Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead. WARNING! Sanding or scraping pressure treated lumber may be hazardous; wear appropriate protection.

Version: 07/2025

LIMITED WARRANTY:  The technical data on this label or on other data is true and accurate to the best of our knowledge.  We guarantee our products to conform to ANCHOR PAINT MFG. CO. quality control standards.  Due to misuse in handling, storage, application and workmanship or variables such as weather or surface integrity that are beyond our control, Anchor Paint does not authorize any representative to make any warranty or merchantability of fitness of this product.  Any liability whatsoever of Anchor Paint Mfg. Co. to the buyer or user of this product is limited to the purchaser’s cost of the product itself.

House and Barn Exterior Acrylic Latex Primer

Product Description

General Description	A pure 100% Acrylic Exterior Latex.  This coating is effective at resisting staining and discoloration caused by tannins in most woods.  Some woods such as redwood and cedar may contain excessive amounts of tannins resulting in stain bleed-through. A second coat of FR3601 may be used in this case. Any tannin bleed should be encapsulated by the first coat and will not bleed into the second.

Common Usage	For use on properly prepared surfaces such as wood, masonry, asphalt, steel, galvanized, and other metals. FR3601 may also be used on other surfaces such as glass, tile, and some plastics.

Color	White

Finish	Low Sheen

Technical Data

Solids by Volume	52.87%

Recommended Thickness	1.6-2.0 mils dry

| Temperature | To Touch | To Recoat |
| --- | --- | --- |
| 75°F / 55% R.H. | 1 hour | 2 hours |

Drying Time

(Cooler temperatures and higher humidity will lengthen drying time)

Architectural and Industrial

Maintenance Category	Primers and Undercoaters

AIM Category VOC Limit	2.9 lb/gal (350 g/l)

Coating VOC	0.41 lb/gal (49 g/l) – Minus Water and Exempt Materials

Material VOC	0.17 lb/gal (20 g/l)

Density	10.85 lb/gal (1300 g/l)

Theoretical Coverage	621 ft2/gallon at 1 mil dry, assuming no application losses.  Coverage will vary depending on color, the surface texture and application technique.

Packaging	5 Gallon pails, 1 Gallon cans, and quart (1/4 gallon) cans

Storage Temperature	Minimum 35°F			Maximum 110°F

| Flexibility: | Excellent | Weather: | Excellent | Abrasion: | Good |
| --- | --- | --- | --- | --- | --- |

Physical Properties

Heat Resistance	120-150°F Continuous

Performance Data

Safety Information	Refer to the Product Data Sheet or Material Safety Data Sheet for safety information.

| Test Method | ASTM Standard | Result |
| --- | --- | --- |
| Freeze/Thaw | ASTM D2243 | Pass – 3 Cycles |
| Heat Stability | ASTM D1849 | Pass – 2 Weeks at 120°F |

Testing Data

Version: 07/2025

LIMITED WARRANTY:  The technical data on this label or on other data is true and accurate to the best of our knowledge.  We guarantee our products to conform to ANCHOR PAINT MFG. CO. quality control standards.  Due to misuse in handling, storage, application and workmanship or variables such as weather or surface integrity that are beyond our control, Anchor Paint does not authorize any representative to make any warranty or merchantability of fitness of this product.  Any liability whatsoever of Anchor Paint Mfg. Co. to the buyer or user of this product is limited to the purchaser’s cost of the product itself.